                            [image: image1.png]INousTRIAL GERAMIC probucTs, INC.




 [image: image2.jpg]




	Physical Properties
	

	Modulus of Rupture
	1100 – 1250 PSI

	Apparent Specific Gravity
	2.2

	Bulk Density
	1.79 g/cm3

	Absorption
	10.6%

	Apparent Porosity
	18.9 %


                                                                                          ICP TECH CENTER

                          Marysville, Ohio
                                                  Production and development of internal cores                                                                  
[image: image3.wmf]
* caustic leeching of ceramic cores requires special chemicals and processing. 

Contact ICP for more information. 1-800-427-2278
  Internal Cores


 


INCORAL ceramic cores


for Aluminum Castings are designed to be easily removed via water blast,


mechanical or caustic leeching*





1-800-427-2278





� HYPERLINK "http://www.industrialceramic.com" ��www.industrialceramic.com�


Fax: 937-644-2646





Typical Chemical Analysis





     Oxide         Weight %





       SiO2                   99.88


       Al2O3           0.086


       TiO2              0.032


       Fe2O3           0.008


 














